Product technical parameters

| Product name | 0.18mm PTFE Film Tape M018H |  |  |
| --- | --- | --- | --- |
| Item | Unit | Product standard | Test standard |
| Adhesive thickness | mm | 0.05±0.01 | GB/T7689.1 |
| Product thickness | mm | 0.18±0.015 | GB/T7689.1 |
| Gram weight | g | 350±15 | GB/T7689.1 |
| Peel strength (90 °test) | N/25mm | ≥6 | ASTM D4851- 88 |
| Initial adhesion (30 ° test) | Steel ball number | ≥19#Steel ball | ASTM D4851- 88 |
| Temperature resistance | ℃ | -40~260℃ | GB/T2423.1 |